SECTION 03 35 00

INTERIOR CONCRETE DUSTPROOFING

*************************************************************************************************************

THIS SPECIFICATION IS PROVIDED BY PROSOCO, INC. AS A SERVICE AND IS INTENDED TO BE USED AS A PROJECT SPECIFIC SPECIFICATION SECTIONS. ONLY LISTED APPLICATORS MAY APPLY THE CONSOLIDECK® HIGH PERFORMANCE CONCRETE FLOOR SYSTEM. CONTACT PROSOCO, INC CUSTOMER CARE at  800-255-4255 FOR A LISTED APPLICATOR.

*************************************************************************************************************

TIPS:

To view non-printing Editor's Notes that provide guidance for editing, click on the Show/Hide button or Word 2010 offers a convenient keyboard shortcut; press the Ctrl+* keystroke to toggle on/off. (Press the Ctrl key, Shift key, and the number 8 simultaneously).

PART 1 GENERAL

1. 01	SUMMARY

  - Section Includes

    - Application of clear reactive, penetrating liquid hardener.

  - Related Sections

    - Section 01 33 00- Submittal Procedures.

    - Section 01 45 80- Testing Laboratory Services.

    - Section 01 60 00- Product Requirements.

    - Section 03 30 00- Cast-in-Place Concrete.

  - REFERENCES

  - Living Building Challenge (LBC) 2.0/2.1.

  - Scientific Certification System (SCS) Indoor Air Quality Gold Certification.

  - NSF International/Nonfood Compound Registration.

  - American National Standard Institute / National Floor Safety Institute ANSI/NSFI B101.1-2009 Test Method for Measuring Wet SCOF of Common Hard-Surface Floor Materials.

  - American Society for Testing and Materials:

    - ASTM C1028 -  Standard Test Method for Determining the Static Coefficient of Friction of Ceramic Tile and Other Like Surfaces by the Horizontal Dynamometer Pull-Meter Method.

    - ASTM D4541 - Standard Test Method for Pull-Off Strength of Coatings Using Portable Adhesion Testers.

    - ASTM E96/96M Method B (Water Method) - Standard Test Methods for Water Vapor Transmission of Materials.

    - ASTM G154 -Standard Practice for Operating Fluorescent Ultraviolet (UV) Lamp Apparatus for Exposure of Nonmetallic Materials.

  - SUBMITTALS

- Product Data and Material Safety Data Sheets:

    - Submit manufacturer’s product data sheets on all products to be used for the work.

      - All specified concrete surface treatments.

- VOC Certification: Submit certification that products furnished comply with regulations controlling use of volatile organic compounds (VOC).

- Test Reports

  - Provide test reports confirming compliance with specified performance criteria.

  - QUALITY ASSURANCE

- Penetrating Concrete Hardener/Densifier Installer Qualifications:

  - Provide letter of completion from chemical manufacturer stating that installer is listed applicator of special concrete finishes, and has completed the necessary training programs at time of Bid and within submittal package.

  - Applicator shall be familiar with the specified requirements and the methods needed for proper performance of work of this section. Applicator must have availability of proper equipment to perform work within scope of this project on a timely basis. Applicator should have successfully performed a minimum of 5 projects of similar scope and complexity.

- Pre-Installation Meeting: Shall convene before the start of work on new concrete slabs and start of application of concrete finish system.

  - Require attendance of parties directly affecting work of this Section, including the Owner’s Representative, Contractor, Architect, concrete installer, and applicator. Meeting should only convene when all parties are present.

  - Review the following:

        - Physical requirements of completed concrete slab and slab finish.

        - Locations and time of test areas.

        - Protection of surfaces not scheduled for finish application.

        - Surface preparation.

        - Application procedure.

        - Quality control.

        - Cleaning.

        - Protection of finish system.

        - Coordination with other work.

- Mock-up shall take place on site, prior to the first application of the densifier.

  - Require attendance of parties directly affecting work of this Section, including the Contractor, Architect, applicator, and Owner’s Representative.

  - Contractor to notify the above parties one week in advance of date and time when mock-up will be completed.

  - Demonstrate the materials, equipment and application methods to be used for work specified herein in pre-approved location approximately 50 sq. ft. in area or as directed by Architect or Owner’s Representative.

  - Retain acceptable mock-up during construction as a standard for judging the completed Work.  Areas may remain as part of the completed work.

  - DELIVERY, STORAGE AND HANDLING

    - Deliver materials in original containers, with seals unbroken, bearing manufacturer labels indicating brand name and directions for storage.

    - Store concrete hardener/densifier in environment recommended on published manufacturer’s product data sheets.

- Store containers upright in a cool, dry, well-ventilated place, out of the sun with temperature between 40 and 100 degrees F (4 and 38 degrees C).

- Protect from freezing.

- Store away from all other chemicals and potential sources of contamination.

- Keep lights, fire, sparks and heat away from containers.

- Do not drop containers or slide across sharp objects.

- Do not stack pallets more than three high.

- Keep containers tightly closed when not in use.

  - PROJECT CONDITIONS

    - Environmental limitations:

      - Comply with manufacturer’s written instructions for substrate temperature and moisture content, ambient temperature and humidity, ventilation, and other conditions affecting performance and finishing requirements.

    - Close areas to traffic during floor application and after application for time period recommended in writing by manufacturer.

    - The completed slab shall be protected to prevent damage by the other trades during floor completion.

    - Temperature Limitations:

      - Do not apply when surface and air temperature are below 40 degrees F (4 degrees C) or above 95 degrees F (35 degrees C) unless otherwise indicated by manufacturer’s written instructions.

      - Do not apply when surface and air temperatures are not expected to remain above 40 degrees F (4 degrees C) for a minimum of 8 hours after application, unless otherwise indicated by manufacturer’s written instructions.

    - Do not apply under windy conditions such that the concrete surface treatment may be blown to surfaces not intended.

    - Do not apply to frozen substrate. Allow adequate time for substrate to thaw, if freezing conditions exist before application.

    - Do not apply earlier than 24 hours after rain or if rain is predicted for a period of 8 hours after application, unless otherwise indicated by manufacturer’s written instructions.

    - Temporary Lighting: Minimum 200 W light source, placed 8 feet (2.5 meters) above horizontal concrete surface for each 425 square feet (40 square meters) of concrete being finished.

    - Temporary Heat: Ambient temperature of 50 degrees F (10 degrees C) minimum.

    - Ventilation: Provide ventilation during coating evaporation stage in confined or enclosed areas in accordance with manufacturer’s instructions.

PART 2 PRODUCTS

  - MATERIALS

    - Pre-Densifier Concrete Cleaner: Shall remove dirt, oil, grease, and other stains from existing slab surface.

      - Consolideck Cleaner/Degreaser manufactured by PROSOCO, Inc., Lawrence, KS, (800) 255-4255, www.prosoco.com, (NO SUBSTITUTE).

      - Auto Scrubber Machine: equipment used for cleaning operations, as required to produce specified results.

    - Penetrating Concrete Hardener/Densifier: Lithium silicate hardener/densifier shall penetrate and react with concrete to produce insoluble calcium silicate hydrate within the concrete pores.  The penetrating concrete hardener shall reduce dusting, increase abrasion resistance and not contribute to surface crazing/surface Alkali Silicate Reactions (ASR).

      - Consolideck LS/CS, manufactured by PROSOCO, Inc., Lawrence, KS, (800) 255-4255, www.prosoco.com, (NO SUBSTITUTE).

      - Subject to compliance with the following requirements:

        - Living Building Challenge 2.0/2.1 Red List Compliant.

        - Recipient of Scientific Certification System (SCS) Indoor Air Quality Gold Certification.

        - Comply with national, state and district AIM VOC regulations and be 50 g/L or less.

        - Registered as an approved NSF International/Nonfood Compound Registration.

        - Abrasion Resistance: >50% improvement over untreated samples when tested in accordance with ASTM C1353.

        - Achieve ‘High Traction Range’ readings when tested in accordance with ANSI B101.1.

        - Coefficient of Friction: >0.60 dry, >0.60 wet when tested in accordance with ASTM C1028.

        - Adhesion:  >10% increase in pull-off strength when compared to an untreated sample when tested in accordance with ASTM D4541.

        - Water Vapor Transmission:  100% retained when compared to untreated samples when tested in accordance with ASTM E96/96M Method B (Water Method).

        - UV Stability:  No degradation or yellowing of material when tested in accordance with ASTM G154.

  - EQUIPMENT

    - Auto Scrubber Machine: equipment used for cleaning operations, as required to produce specified results.

PART 3 EXECUTION

  - EXAMINATION

- Examine substrate with installer present for conditions affecting performance of finish. Correct conditions detrimental to timely and proper work. Surfaces that are in question or that will affect the execution or quality of work must be brought to the attention of the Owner’s Representative before work may begin.

  - PREPARATION

- Clean dirt, dust, oil, grease and other contaminants that interfere with penetration or performance of specified product from surfaces.

Retain first paragraph below if concrete surface will be cured prior to application of hardener/densifier.

- Remove remnants of curing compound, bond breaker, and construction laitance prior to application of densifier. Remove by cleaning and scrubbing in accordance with manufacturer's instructions.

- Repair, patch and fill cracks, voids, defects and damaged areas in surface as approved by the Architect. Allow repair materials to cure completely before application of product.

- Scrub floor with pre-densifier floor cleaner to remove latent salts.

- Do not proceed until unsatisfactory conditions have been corrected.

  - GENERAL REQUIREMENTS

- Include all work necessary to achieve desired final finish.

  - APPLICATION CONCRETE HARDENER/DENSIFIER

Retain one of the two paragraphs below depending on application sequence

Retain paragraph below to suit Project where application will occur on freshly placed, uncured steel troweled concrete; delete if not required

- Freshly Placed, Uncured Steel Troweled Concrete:  Concrete:  Apply concrete hardener/densifier after final concrete finishing and final soft cut control joints.  Apply according to manufacturer’s written instructions and as follows:

  - Clean concrete of any dirt/residue of soft cut saw debris.

  - Apply hardener/densifier per manufacturer’s recommended application rate to designated finished floor area, with a low pressure sprayer fitted with a 0.5 gpm spray tip.

  - Apply sufficient material to wet the surface without producing puddles.  Use a clean soft-bristle push broom or microfiber pad to spread the hardener/densifier evenly to achieve uniform wetting.  Avoid spreading once drying begins.  Surface should remain wet for 5-10 minutes.  Avoid over-application.  (Scrubbing is not necessary.)

  - Allow treated surfaces to dry.

  - Immediately apply the specified curing compound or initiate the specified curing procedure.

Retain paragraph below to suit Project where application will occur to cured steel troweled concrete; delete if not required.

- Cured Steel Troweled Concrete:  Apply concrete hardener/densifier to cured steel troweled concrete.  Apply according to manufacturer’s written instructions and as follows:

- Remove remnants of bond breakers, curing agents, surface grease and oil and construction debris.  Contact PROSOCO, Inc. at 800-255-4255 to obtain manufacturer recommended cleaner and cleaning method.

- Apply hardener/densifier per manufacturer’s recommended application rate to designated finished floor area, with a low pressure sprayer fitted with a 0.5 gpm spray tip.

- Apply sufficient material to wet the surface without producing puddles.  Use a clean soft-bristle push broom or microfiber pad to spread the hardener/densifier evenly to achieve uniform wetting.  Avoid spreading once drying begins.  Surface should remain wet for 5-10 minutes.   Avoid over-application.  (Scrubbing is not necessary)Allow treated surface to dry.

- Once thoroughly dry, concrete may be auto-scrubbed, buffed or burnished.  Buffing or burnishing should be performed with the appropriate pad.

  - SLAB PROTECTION

- Protect finished floors to prevent damage including staining, gouges and scratching by construction traffic and activities until possession.

- Do not drag or drop equipment or material across the slab which will scratch or chip it.

- Tires shall be inspected for debris prior to use on slab. Remove embedded items which may cause damage to floor slab. .

- Clean up spills on slab immediately. Provide cleaning chemicals and absorptive materials.

- Develop a concrete protection procedure which addresses the following procedures:

  - Communication of protection plan to subcontractors and vendors.

  - Procedures for cleaning up slab spills, including use of and availability of cleaning chemicals and absorptive materials at Site.

  - Contact PROSOCO, Inc. at 800.255.4255 to obtain manufacturer recommended Concrete Floor Protection Plan, if necessary.

- Provide a clean slab surface at all times using approved concrete maintenance cleaner within an auto scrubber, equipped with soft nylon brushes, in accordance with manufacturer's recommendations.

END OF SECTION